**FRESCOLORI Concrete Five S (sanded)**

Delivery and servicing surfaces exclusively by trained FRESCOLORI processing specialists, with a long-term guarantee of high quality.

Concrete Five S, an extension of our concrete surface, obtained by adding additional coarse marble granules. A spatial experience of the concrete surface. The tensioned interaction of the opposites - cold and warm, smooth and structured, dense and porous. An individual statement, a space statement: timeless modernity, solid and stable. An effect that cannot be more immediate that now.

**FRESCOLORI Concrete Five S (sanded)**

Material: 2 CM5K layers

ETC

Consumption: CM5K about 2.4 kg/m² each layer

ETC, about 0.08kg/m²

Colour : freely selectable

Application: Indoor

Surfaces are prepared and primed.

* Application of the first layer of the Caramor limestone-marble plaster, in grain thickness 5, with added coarse marble granules
* Respect the waiting times with a rest period until the next day
* Application of the second layer of the Caramor limestone-marble plaster, in grain thickness 5, with added coarse marble granules
* Direct structuring during application, alternatively with the aid of easy application of the material
* Observe the quite short waiting time (touch dry)
* Humidify the surface with a long bristle brush/spray bottle with water, and prevent any running of the water on the surface
* Instant smooth the surface with a trowel, by applying a uniform pressure
* Observe the uniform distribution of the effluent limestone milk
* Respect a waiting time of one day (until the next day)
* Polish the surface with the polishing machine (grain size 180)
* Apply the ETC protection with a brush