**FRESCOLORI Rock**

Delivery and servicing surfaces exclusively by trained FRESCOLORI processing specialists, with a long-term guarantee of high quality.

A differently raised, large-area structured surface - powerful and massive. With the natural radiance of a rocky terrain.

**FRESCOLORI Rock**

Material: 1 CM7 layer

Wax

Consumption: CM7 about 1.5 kg/m² each layer

Wax, about 0.11 kg/m²

Colour : freely selectable

Application: Indoor

Surfaces are prepared and primed.

* Apply the Caramor limestone-marble plaster in grain thickness 7
* Observe the quite short waiting time (touch dry)
* Humidify the surface with a long bristle brush/spray bottle with water, and prevent any running of the water on the surface
* Instant smooth the surface with a trowel, by applying a uniform pressure
* Observe the uniform distribution of the effluent limestone milk
* Smooth the surface with a trowel
* Pulling the material upwards (suction effect)
* Respect the waiting times with a rest period until the next day
* Easily grind corners and edges
* Apply the wax with a trowel
* Apply instant removal of excess wax with rags
* Observe the waiting time of about 3 hours
* Polish the surface with a polishing machine provided with a lambskin covered disc