**FRESCOLORI Structure Seven L**

Delivery and servicing surfaces exclusively by trained FRESCOLORI processing specialists, with a long-term guarantee of high quality.

A matte open-pore surface, which gains expression through our Caramor in grain strength 7 and by a lively application. Densely compressed areas give the surface its character, more or less.

**FRESCOLORI Structure Seven L**

Material: 1 CM7 layer

Consumption: CM7 about 1.3 kg/m² each layer

Colour : freely selectable

Application: Indoor

Surfaces are prepared and primed.

* Apply the Caramor limestone-marble plaster in grain thickness 7
* Observe the quite short waiting time (touch dry)
* Humidify the surface with a long bristle brush/spray bottle with water, and prevent any running of the water on the surface
* Instant smooth the surface with a trowel, by applying a uniform pressure
* Observe the uniform distribution of the effluent limestone milk
* Freedom of design: Application of the plaster in wild lively optics, with a moving line imprinting the surface image